Date:

To

_______________

_______________

Sub:  	A) Minimum Testing of Concrete and Steel for ensuring Strength, Quality and Durability of concrete.

B) Continues Supervision

C) Additional Testing for Durability

Project:  __________________________________________________________________

Dear Sir,

We thank you for appointing us as  `Consulting Structural Engineers ` for the above project, we are sure that we will discharge our duties satisfactorily so as to design a Safe, Stable And Durable structure for you.

A) Minimum Testing - Please note that our structural design is based on the governing code, IS456:2000, the Code of practice for Plain and Reinforced Concrete.

Implementation of the provisions of the code ensures desired quality Concrete, provided following specified tests are done primarily on Concrete, Steel, Water and other Raw Materials.

As a responsible user, you need to get following Tests done at given frequency:

  - Table 1 - Concrete Cube Testing:

| Quantity of Concrete in the work, m3 | Number of samples | Frequency - The minimum frequency of sampling of concrete of each grade shall be in accordance with IS 456: 2000, as given in Table 1: (One sample consists of sets of 3 cubes; two sets are required one for 7 days and one for 28 days.) |
| --- | --- | --- |
| 1-5 | 1 |  |
| 6-15 | 2 |  |
| 16-30 | 3 |  |
| 31-50 | 4 |  |
| 51 and above | 4 plus one additional for each additional 50 m3 |  |
| Note: At least one sample taken from each shift where concrete is produced at continuous production unit, such as ready – mixed concrete plant, frequency of sampling may be agreed upon mutually suppliers & purchaser. |  |  |

- Water Quality- Frequency – Every month and change of source.

| Sr No. | Test for | Tested as per | Permissible Limit Max |
| --- | --- | --- | --- |
| i | Organic | IS 3025 (Part 18) | 200 mg/l |
| ii | Inorganic | IS 3025 (Part 18) | 3000 mg/l |
| iii | Sulphates (as SO3) | IS 3025 (Part 24) | 400 mg/l |
| iv | Chlorides (as Cl) | IS 3025 (Part 32) | 2000 mg/l for concrete not containing embedded steel and 500 mg/l for reinforced concrete work. |
| v | Suspended matter | IS 3025 (Part 17) | 2000 mg/l |
| VI | pH | IS 3025 | 6-8 |

- Steel (IS 1786 - 1985) : Frequency – One sample of every diameter from each lot

Mechanical properties of High Strength Deformed Bars and wires

| SL.No. | Property | Grade |  |  |
| --- | --- | --- | --- | --- |
|  |  | Fe 415 | Fe 500 | Fe 550 |
| 1 | 2 | 3 | 4 | 5 |
| i | 0.2 percent proof stress / yield stress, Min, N/mm2 | 415.0 | 500.0 | 550.0 |
| ii | Elongation percent, Min, on gauge length 5.65√A, where A is the cross sectional area of the test piece. | 14.5 | 14.5 | 14.5 |
| iii | Tensile strength, Min | 10 percent more than the actual 10.2 percent proof stress but not less than 485.0 N/mm3 | 8 percent more than the actual 0.2 percent proof stress but not less than 545.0 N/mm3 | 6 percent more than the actual 0.2 percent proof stress but not less than 585.0 N/mm3 |

Note; Bend & Re-bend test for steel to be done at site and if not possible at laboratory

It is very much essential to carry out all the above tests and send the results to us for our information and records on regular basis.

B) Continues Supervision -

Please note it is essential to appoint a Full Time Civil Engineer or Project Management Consultant for supervision of work, who that will be responsible to carry out all the desired tests and also other aspects of good concrete - Batching, Transportation, Placing, Compaction and Curing.

You have two options for producing Concrete:

- Site mix Concrete: It is advisable to appoint an agency to carry out Mix Design after carrying out all the tests on raw materials and issue the same for implementation to site engineer. The site should have a laboratory set up for testing of moisture content of sand, silt content of sand, cube testing machine, slump test cone or flow table and sieve set for sieve analysis.

- Ready Mix Concrete: Responsibility of carrying out the mix design (and tests on raw material prior to that) is shifted to RMC supplier.  QCI certification of suppliers’ plants adds to confidence..

C) Additional Testing for Durability –

It is noted that RCC structures built on seashores are venerable to Sulphate and Chloride attack and are deteriorating at much faster rate. Many a times structure shows corrosion cracks within 3 to 5 yrs.

We strongly recommend use of High Performance Concrete (Performance against water & chloride penetration). Additional tests & corresponding remedial measures for HPC are required to carry out, which we may suggest from time to time. All the tests are listed in Annexure 1.

It is important to note that Structure will be safe, stable and durable only when all above mentioned points:

A) Minimum Testing of Concrete and Steel for ensuring Strength, Quality and Durability of concrete., B) Continues Supervision, C) Additional Testing for Durability are taken care of.

Regards,

For Epicons Consultants Pvt. Ltd.

ANNEXURE 1

Parameters for approval of High Performance Concrete, Trial mixes

- RCPT (Chloride Permeability) to ASTM C1202:

- Maximum Charge Pass (Coulombs) at 28 days

- Concrete with OPC – 2000 max

- Concrete with fly ash- 1800 max

- Concrete with GGBS- 1500 max

- Initial Surface Absorption to BS 1881 Part 208:1996

- ISAT at 28 days: 	10 minute test

- Concrete of all types                                           	 0.25ml/m2/sec

- Water Permeability to DIN 1048:

- Maximum Penetration (mm) at 28 days

- Concrete of types                                             	25 mm

- Minute Absorption to BS 1881 Part 122:

- 30 minute absorption, 28 days

- Concrete of all types                                            2.5% at 28 days

- Drying Shrinkage IS:1199 ( ONLY FOR HIGH RISE BUILDINGS)

- Concrete all types                                             	  0.05%

- Moisture movement IS:1199 (ONLY FOR HIGH RISE BUILDINGS)

- Concrete all types                                            	 0.03%